MACFLO SLIDE VALVE

PVC Gate Valve

Please turn over page for Spec Sheet Description: - Size: 1 1/4’’-6’’(DN32-DN150) - Standard: DIN,ANSI,BS - Material: UPVC - Working Pressure: 0.35mpa - Widely used in effluent applications..

Materials of Construction

No.; Parts; Material. 1; Faucet; UPVC. 2; Valve Gate; PP, 1Cr13. 3; Seat; EPDM,NBR. 4; Bolt; A2. 5; Stem; 1Cr13. 6; Body; UPVC. 7; Cap; UPVC. 8; O-Ring; EPDM,NBR. 9; Bushing; UPVC. 10; Key; UPVC. 11; Handle; ABS,ZL106.

Dimension

Size; A; B; DN; Φ; L; H; PN. mm(in); (Mpa). 1 1/4''; 143; 115; 32; 40; 68; 57; 0.35. 1 1/2''; 170; 136; 40; 50; 100; 74; 0.35. 2''; 207; 163; 50; 63; 108; 86; 0.35. 2 1/2''; 240; 190; 65; 75; 125; 104; 0.35. 3''; 305; 222; 80; 90; 128; 150; 0.35. 4''; 350; 260; 100; 110; 132; 170; 0.35. 6''; 505; 380; 150; 160; 172; 242; 0.35.